Исследование пространственной спин-модулированной структуры серии

Bi1-xLaxFeO3 с помощью ядерно-резонансных методов

Гунбин А.В.

аспирант1

Гервиц Н.Е.

Научный сотрудник1

Ткачев А.В.

Старший научный сотрудник1, к.ф.-м.н.

Журенко С.В.

Младший научный сотрудник1, студент2

1Физический Институт Академии Наук им. Лебедева, Москва, Россия

2Физический факультет МГУ им. Ломоносова, Москва, Россия

ngervits@gmail.com

Перспективы использования мультиферроика 1 типа BiFeO3в спинтронике, для хранения информации и в различных мультифункциональных устройствах вот уже более 30 лет привлекают к нему пристальное внимание [1]–[4]. В 1982 году с помощью нейтронов было обнаружено наличие пространственной спин-модулированной структуры (ПСМС) с периодом λ = 620 ± 20 Å[5]. Для применения соединения в практических целях, оказалось необходимым разрушить ПСМС для возможности использования уникальных магнитных свойств феррита висмута [6].

Для разрушения ПСМС в разное время разными авторами были предложены такие варианты как замещение висмута редкоземельными элементами [7]–[9], синтезпленокикристалловвнано размере[2], [10]–[12], воздействие внешним полем[13].

Одним из наиболее эффективных и наглядных методов наблюдения ПСМС является ЯМР-спектроскопия. На ЯМР-спектрах в случае наличия ПСМС циклоидного типа мы наблюдаем характерных «двурогий» спектр размахом до 2 МГц, который аппроксимируем в соответствии с литературой [14] и получаем в числе прочих данных параметр ангармонизма m, являющийся важной характеристикой состояния магнитной структуры.

Другим эффективным методом является Мессбауэровская спектроскопия, с последующей обработкой экспериментальных спектров в программе SpectrRelax[15].

Данное исследование посвящено влиянию гомовалентного замещения висмута  лантаном на ПСМС в ромбоэдрической фазе R3c системы Bi1-xLaxFeO3 с x = {0, 0.015, 0.03, 0.05 и 0.10} с помощью ЯМР-спектроскопии в нулевом поле при Т = 4,2 К и с помощью Мессбауэровской спектроскопии при Т = 300 К.

При проведении измерений были получены ЯМР (при 4,2 К) и Мессбауэровские (при 300 К) спектры всех образцов. Для всех спектров вплоть до 10% замещения лантаном ЯМР спектроскопия демонстрирует наличие двугорбой структуры и подтверждает наличие ПСМС. При 25% замещении оба метода наблюдают отсутствие ПСМС.С помощью ЯМР-спектроскопии обнаружена дополнительная высокочастотная линия, интенсивность которой зависит от степени замещения лантаном. Было обнаружено уменьшение параметра ангармонизма при обеих температурах при увеличении степени замещения лантаном.

Исследование выполнено при финансовой поддержке РФФИ в рамках научного проекта №17-52-80036 БРИКС_а.

[1]	A. M. Kadomtseva, Y. F. Popov, A. P. Pyatakov, G. P. Vorob’Ev, A. K. Zvezdin, and D. Viehland, “Phase transitions in multiferroic BiFeO3 crystals, thin-layers, and ceramics: Enduring potential for a single phase, room-temperature magnetoelectric ‘holy grail,’” Phase Transitions, vol. 79, no. 12, pp. 1019–1042, Dec. 2006.

[2]	S. V Khikhlovskyi, G. Blake, and S. VVKhikhlovskyi, “The renaissance of multiferroics: bismuth ferrite (BiFeO 3 )-a candidate multiferroic material in nanoscience,” 2010.

[3]	G. Catalan and J. F. Scott, “Physics and Applications of Bismuth Ferrite,” Adv. Mater., vol. 21, no. 24, pp. 2463–2485, Jun. 2009.

[4]	M. Bibes and A. Barthélémy, “Multiferroics: Towards a magnetoelectric memory,” Nature Materials, vol. 7, no. 6. Nature Publishing Group, pp. 425–426, 2008.

[5]	I. Sosnowska, T. P. Neumaier, and E. Steichele, “Spiral magnetic ordering in bismuth ferrite,” J. Phys. C Solid State Phys., vol. 15, no. 23, pp. 4835–4846, 1982.

[6]	Y. POPOV, A. ZVEZDIN, G. VOROBEV, A. KADOMTSEVA, V. MURASHEV, and D. RAKOV, “LINEAR MAGNETOELECTRIC EFFECT AND PHASE-TRANSITIONS IN BISMUTH FERRITE, BIFEO3,” JETP Lett., vol. 57, no. 1, pp. 69–73, 1993.

[7]	A. M. Kadomtseva, Y. F. Popov, G. P. Vorob’ev, and A. K. Zvezdin, “Spin density wave and field induced phase transitions in magnetoelectric antiferromagnets,” Phys. B Phys. Condens. Matter, vol. 211, no. 1–4, pp. 327–330, May 1995.

[8]	Y. Popov, A. Zvezdin, G. Vorbev, V. M.-J. Lett, and  undefined 1993, “Linear magnetoelectric effect and phase transitions in bismuth ferrite, BiFeO3,” jetpletters.ac.ru.

[9]	C. Tab Ares-Muñoz, J. P. Rivera, A. Bezinges, A. Monnier, and H. Schmid, “Measurement of the quadratic magnetoelectric effect on single crystalline bife03,” Jpn. J. Appl. Phys., vol. 24, pp. 1051–1053, 1985.

[10]	F. Huang et al., “Peculiar magnetism of BiFeO3 nanoparticles with size approaching the period of the spiral spin structure,” Sci. Rep., vol. 3, 2013.

[11]	F. Zavaliche et al., “Multiferroic BiFeO3 films: Domain structure and polarization dynamics,” Phase Transitions, vol. 79, no. 12, pp. 991–1017, Dec. 2006.

[12]	C. Y. Kuo et al., “Single-domain multiferroic BiFeO 3 films,” Nat. Commun., vol. 7, Sep. 2016.

[13]	G. Le Bras, D. Colson, A. Forget, N. Genand-Riondet, R. Tourbot, and P. Bonville, “Magnetization and magnetoelectric effect in Bi1-x Lax FeO3 (0≤x≤0.15),” Phys. Rev. B - Condens. Matter Mater. Phys., vol. 80, no. 13, Oct. 2009.

[14]	A. V. Zalessky, A. A. Frolov, T. A. Khimich, A. A. Bush, V. S. Pokatilov, and A. K. Zvezdin, “57Fe NMR study of spin-modulated magnetic structure in BiFeO3,” Europhys. Lett., vol. 50, no. 4, pp. 547–551, May 2000.

[15]	V. S. Rusakov et al., “Spatial spin-modulated structure and hyperfine interactions of 57Fe nuclei in multiferroics BiFe1–x T xO3 (T = Sc, Mn; x = 0, 0.05),” Phys. Solid State, vol. 58, no. 1, pp. 102–107, Jan. 2016.