A novel functional material made of a light-responsive chiral nematic liquid crystal structured at the micron level

A.O. Piven, D.D. Darmoroz, T. Orlova.

First-year Master's student

National Research ITMO University, School of Life Sciences, St. Petersburg, Russia

E-mail: piven@infochemistry.ru

Currently, it is widely known that liquid crystal materials are able to demonstrate various types of orientation defects in a partially ordered molecular field. Liquid crystal structures with such defects have non-trivial optical properties useful for technological applications in optics and photonics. On the other hand, such defects cannot be obtained by a continuous change of the liquid crystal material ordering, that also opens prospects for using such structures for recording and storing information at the molecular level [1].

In previous studies, the creation of localized static defect structures in thin films of frustrated chiral nematic liquid crystals was demonstrated by optically induced reorientation of liquid crystal molecules by both structured and Gaussian light beams [5, 7]. A recent approach based on light-induced control of cholesteric helix allows to generate multiple localized static structures as well as a unique dynamic revolving pattern by an ultraviolet Gaussian beam with a beam power of only tens of nW [6]. Our research is aimed at a detailed study of the relationship between the structure and behavior of light-induced localized supramolecular patterns in the thin films of frustrated chiral nematics with controlling the spatiotemporal characteristics of a recording Gaussian light beam.

In this talk, we demonstrate a set of static and dynamic localized twisted structures in thin films of a light-responsive chiral nematic liquid crystal by optically induced photochemical transformations of chiral dopant molecules. Light illumination of the frustrated chiral liquid crystal with a Gaussian beam enables local winding of cholesteric helix and formation of static and dynamic liquid crystal structures with a size of 10-100 microns. The high relevance of our study is ensured by intensive scientific and technical developments in the field of adaptive optical elements for photonic devices and light structuring systems [2, 4], as well as elements for transporting micro- and nanoparticles [3, 6].

Acknowledgement. This work was financially supported by the Government of the Russian Federation through the ITMO fellowship and professorship program.

Литература

- Ackerman, P.J. Two-dimensional skyrmions and other solitonic structures in confinement-frustrated chiral nematics / P.J. Ackerman, R.P. Trivedi, B. Senyuk, J. Lagemaat, I.I. Smalyukh // Physical Review E. 2014, №90.

- Ackerman, P.J. Optical generation of crystalline, quasicrystalline, and arbitrary arrays of torons in confined cholesteric liquid crystals for patterning of optical vortices in laser beams / P.J. Ackerman, Z. Qi, I.I. Smalyukh // Physical Review E. 2012, №86.

- Evans, J.S. Optical generation, templating, and polymerization of three-dimensional arrays of liquid-crystal defects decorated by plasmonic nanoparticles / J.S. Evans, P.J. Ackerman, D.J. Broer, J. Lagemaat, I.I. Smalyukh // Physical Review E. 2013, №87.

- Hess, A.J. Control of Light by Topological Solitons in Soft Chiral Birefringent Media / A.J. Hess, G. Poy, J.B. Tai, S. Zumer, I.I. Smalyukh // Physical Review X. – 2020, №10.

- Loussert, C. Multiple chiral topological states in liquid crystals from unstructured light beams / C. Loussert, E. Brasselet // Applies Physics Letters. 2014, №104(5). p 1911–1914.

- Orlova, T. Revolving supramolecular chiral structures powered by light in nanomotor-doped liquid crystals / T. Orlova, F. Lancia, C. Lossert, S. Lamsaard, N. Katsonis, E. Brasselet // Nature Nanotechnology. 2018, №13. p. 304–308.

- Smalyukh, I.I. Three-dimensional structure and multistable optical switching of triple-twisted particle-like excitations in anisotropic fluids / I.I. Smalyukh, Y. Lansac, N.A. Clark, R.P. Trivedi // Nature Materials. 2010, №9. p. 139–145.